## Slide 1: 3D Carbon Nanotubes for Infrared Sensing
Sammy Mahdi, Nanomanufacturing Group
04/10/2018
Sensors Cafe
Notes: Hi everyone, I’m Sammy and my phd is about developing infrared sensors using carbon nanotubes, one of the most common applications of infrared sensing is thermal.

## Slide 2: Infrared Sensors
Notes: Imagine you are an autonomous vehicle and this is what you see during the night, obviously there is not much information there, however if you look at the infrared spectrum, there is so much more.

## Slide 3: Black Body Radiation
Notes: So why is there more information in the second photo, it turns out that every object that has a temperature above 0 K, emits energy in the infrared band, so the second image is created by measuring the temperature of the object ahead which is invariant of lighting conditions.

## Slide 4: IR Detectors Types
Cooled IR sensors
+ High sensitivity
+ Excellent resolution
High power consumption
Expensive/bulky
Uncooled IR sensors
+ Low power consumption
+ Cheap/portable
Less sensitive
Low response time

## Slide 5: IR Microbolometer
T
IR Wave
Change in T
Measure T
Notes: Infrared radiation is also know as thermal radiation, if we have an object that absorbs the infrared radiation, then it’s temperature would increase. If our object also changes its electrical properties with the increase of temperature, then we can relate the temperature change to the infrared radiation. One way to construct such device is shown on the figure, you have an IR absorbing membrane and a thermistor which are attached through very thin legs to two electrodes, the reason why the membrane is suspended is so that the temperature change stays in the membrane and is not dissipated to the substrate. In the case of my devices, the CNTs would both function as an IR absorbing membrane and a thermistor.

## Slide 6: Carbon Nanotubes
Advantages
+ Excellent IR absorption
+ Excellent thermal conductivity
+ Low thermal mass
+ Excellent electrical properties
+ Mechanically robust
+ Complex 3D structures
+ Different functionalization
Notes: As Kate mentioned previously, CNTs are amazing materials that can be used in variety of applications, the properties in which I am interested is basically all of them.

## Slide 7
CNT as IR sensors
Excellent IR absorption
Low thermal
mass
Bolometer
3D structures
Notes: The reason why CNTs can make good IR sensors is the following, they have excellent IR absorption. In addition, they have low thermal mass which means that the response time of my sensors can be very low and finally we can structure them in 3D shapes thus maximising the absorption area.

## Slide 8: Current progress on CNT IR sensors
Notes: There is some progress on CNT infrared sensor but most work has been done as a proof of concept and is not easily scalable. You can see some of the crude devices here.

## Slide 9: Desired final device
Notes: We envision the final device to look something like where we have an array of individual sensors

## Slide 10: Photolithography Mask
Notes: In order to fabricate the devices, we have to use lithography techniques, I won’t go into detail on how photolithography works but the first I had to do was to design a mask. The mask is essentially the blueprint for my devices, after I have the blueprint I would expose the patterns on silicon wafer and grow the carbon nanotubes.

## Slide 11: Suspended CNT bridges
Pattern electrodes
Pattern catalyst
CVD growth
Notes: So how do you grow nanotubes? It’s very similar to growing a plan, first you need a soil, in our case we have two different soils – red one and green one, after that we need to put the seeds which is the catalyst (yellow in our schematic), after that we keep them warm at around 800 degrees and we feed them various gasses and from the catalysts we start seeing forests of carbon nanotubes. Something very interesting happens if you plant seeds on two different soils

## Slide 12: Suspended CNT bridges
Two-sided bridge
One-sided bridge
“Flowers”
“Crabs”
Feature | Overlap | Film widths | W/L ratios
Two-sided-bridge | 20 – 80% | 3 μm, 5μm, 7μm 10 μm, 20 μm | 1, 2, 4
One-sided bridge | 20 – 80% | 3 μm, 5μm, 7μm 10 μm, 20 μm | 1, 2, 4

## Slide 13: Double-sided bridges

## Slide 14: Double sided bridges

## Slide 15: Single sided bridges

## Slide 16: Single sided bridges

## Slide 17: Single sided bridges

## Slide 18: Flopped CNT bridges
One-sided flop
Two-sided flop

## Slide 19: Flopped structures

## Slide 20: Flopped structures

## Slide 21: Flopped structures

## Slide 22: Test setup

## Slide 23: Test setup

## Slide 24: Electrical characterization

## Slide 25
Single Sided | T: 10 um L: 20 um

## Slide 26: Single Sided | W: 5 um L: 10 um

## Slide 27: Single Sided | W: 3 um L: 6 um

## Slide 28: Annealing test

## Slide 29: Annealing experiment

## Slide 30: IR response
OFF
ON
OFF
OFF
OFF
OFF
ON
ON
ON

## Slide 31: IR Response | Fourier transform

## Slide 32: Future steps
Improve IR characterization setup
  Focusing lens/high power source
Test double sided bridges
Get better idea about TCR variations across samples
Improve TCR
  Vary growth temperature (different quality CNTs)
  Functionalize with polymers/metal oxides
  Reduce 1/f noise
Design new mask with 8x8 arrays

## Slide 33: Acknowledgements
NanoManufacturing Group

## Slide 34: Summary
Device Concept
Thermal Camera
Fabrication process
Successful device
Array of devices

## Slide 36: Unique features generator
Sweeps catalyst/electrode overlap %
Sweeps film
thickness

## Slide 37: Future work
Finish mask and send for fabrication
Build IR test setup
Get training on lithography
Optimize lithography
Optimize growth
Test devices
Mask v2.0

## Slide 38: Proposed device #2
Honeycombs between electrodes
Functionalize with
polymers
Improved
TCR

## Slide 39: Proposed method #1
Notes: Talk about the advantages of the bridges

## Slide 40: IR Uncooled Microbolometer
– change in temperature
𝜂 – absorption coefficient
– optical power falling on detector
G – thermal conductivity to substrate
– is angular frequency of modulation
= C/G, response time where C is
heat capacity of the detector
– signal output
– detector resistance
– bias current
– temperature coefficients of resistance (TCR)

## Slide 41: IR Detectors Types
Cooled IR sensors
+ High sensitivity
+ Excellent resolution
High power consumption
Expensive/bulky
Uncooled IR sensors
+ Low power consumption
+ Cheap/portable
Less sensitive
Low response time
Notes: Two different types, initially cooled IR sensors,

## Slide 42: Thermal Imaging
Fever screening at airports
Measuring
building efficiency
Harsh conditions/night imaging
Notes: Applications …

## Slide 43: Black Body Radiation
Notes: Every object above 0 K emits EM, the intensity of the radiation is a function of the temperature of the object and the wavelength of the radiation